¤8¤P1 – 163 – C

¤

PROCESSING AND MAGNETIC PROPERTIES OF BIOCERAMICS

Th. Leventouri*, A.C. Kis, K. Sorge1, C. E. Bunaciu, and J. R. Thompson1

Physics Department, Florida Atlantic University, Boca Raton, FL 33431, USA

1Solid State Division, Oak Ridge National Laboratory, Oak Ridge, TN 37830-6061, U.S.A, and

Department of Physics, University of Tennessee, Knoxville, TN 37996-1200, U.S.A.

Bioactivity of ferromagnetic glass-ceramics originates from the calcium phosphate that forms apatite in a physiological environment. Their magnetic properties have been shown to be effective in hyperthermic treatment of animal bone cancer. Correlations between processing, structure, and magnetic properties are presented. A series of samples in the system 45(CaO, P2O5) ySiO2 xFe2O3 were synthesized with varying the processing parameters. X-ray powder diffraction reveals a strong effect of the processing parameters on the qualitative and the quantitative composition of the samples. They all are multiphase systems of 3 or 4 phases. The major phase is calcium phosphate, while hematite and/or magnetite determine their magnetic properties. Magnetic measurements illustrate a strong dependence of the saturation magnetization and hysteresis loss of the biomaterial from the processing parameters. A systematic study of the physical properties in series of ferromagnetic bioceramics is in progress.

$

* Corresponding author: e-mail: leventou@fau.edu